## Slide 1: Plastic Manufacturing Processes
Plastic Conversion Processing
Notes: Introduction
Welcome
Background to FPC
Important contribution to the food industry

## Slide 2: Plastic Types
Thermoplastic polymers
  Polyethylene, Polyester, Polyamide
Elastomers
  Rubbers, Silicones
Thermosetting polymers
  Epoxies, Polyesters,

## Slide 3: Introduction to Plastic Conversion

## Slide 4: Elementary Conversion Process
Solids handling
Mixing
Drying
Melting
Mixing
Pressurisation & pumping
Devolatizing & Stripping

## Slide 5: Finishing Conversion Processes
Die forming
Moulding & Casting
Mould Coating
Secondary shaping

## Slide 6
Properties
Processes
Polymers

## Slide 7: Process selection
Technical Issues
  Dimension tolerance, wall thickness, polymer, size, geometry
Economic Issues
  Number requires, finished cost, tooling cost, production rate

## Slide 8: Material Preparation
Drying
Additives

## Slide 9: Drying
Some polymers really adsorb moisture
  Nylon 2.5% @50%rh 23oC
Moisture can reduce intrinsic viscosity (IV)
Dehumidification driers
  Regeneration to reduce energy
  Temperature must not melt polymer

## Slide 10: Additives
  Heat stabilisers
  Antioxidants
  UV stabilisers & Inhibitors
  Slip agents
  Anti-static agents
  Anti-blocking agents
  Anti-fog agents
  Colours
  Plasticisers

## Slide 11: Additives
Masterbatch
  Concentrated mix of polymer carrier and active ingredient
  Polymer Specific Masterbatch
  Universal Masterbatch

## Slide 12: Mixing
Little mixing in single screw extruders
Mixing initiated in hopper or in batches before being feed into hopper

## Slide 13: Extrusion

## Slide 14: Processes
Extrusion
  profile
  cast sheet and film
  blown film
  co-extrusions

## Slide 15: Extruder Operation

## Slide 16: Extruder Screws

## Slide 17: Extrusion
Heat generated from overcoming friction
Screw profiles designed for each polymer
Little mixing in single screw extruders
Usually continuous process

## Slide 18: Profile extrusion
Profile die fitted to end of extruder to shape melt.
Die swell and profile thinning
Knit lines can be source of weakness
Applications
  Mastic tubes, sweat tubes

## Slide 19: Profiles

## Slide 20: Die Swelling
extrudate swell (youtube.com)

## Slide 21: Die Swelling

## Slide 22: Sheet and cast film extrusion
Profile extrusion with an adjustable slot die
Sheet extruded onto chilled casting rollers
  Rapid cooling of thin sheet
Thick, uneven edges trimmed off
Limit gauge bands
  Windup rollers oscillated or automatic thickness control

## Slide 23: Sheet die

## Slide 24: Cast Film Extrusion Line

## Slide 25: Orientation
Orientation of molecules in one or more directions
Can cause desirable and undesirable changes in the properties of the material.

## Slide 26: Orientation
Achieved by stretching the material at a temperature between Tg and Tm and cooling to lock in orientation.
Film may shrink if subjected to temperatures similar to those at which the orientation took place.

## Slide 27: Orientation of cast film

## Slide 28: Orientation of cast films

## Slide 29: Blow Film Extrusion
Similar to profile extrusion
Produce tube of molten polymer which is inflated with air and air cooled.
Difficult to control melt drawing
Tube collapsed, slit and rolled
Controlled windup speed and bubble pressure

## Slide 30: Blown Film

## Slide 31: Blown Film
BOPP Process - YouTube

## Slide 32: Blown Film Die

## Slide 33: Blown Film External Cooling

## Slide 34: Blown Film Internal Cooling

## Slide 35: Measurements
Blow Up Ratio (BUR)
Draw Down Ratio (DDR)
Effect
  Gauge
  Orientation

## Slide 36: Co-Extrusion
Produce combination of two or more materials
Enable thin barrier layers to be included in materials
Process scrap not recyclable

## Slide 37: Co Extrusion Sheet Die

## Slide 38: Co-Extrusion Blown Film Dies

## Slide 39: Injection Moulding

## Slide 40: Plastic Injection Molding
High pressure melt forced enclosed to closed mould
Mould cavity approximately same shape as item
Produce complex products in single process

## Slide 41: Injector

## Slide 42: Toggle Switch

## Slide 43: Mould

## Slide 44: Mould design
Heavy to withstand pressure
Permit air removal
Avoid unequal cross-section
Provide balanced flow
Avoid weld lines in stressed areas

## Slide 45: Multi Cavity Moulds

## Slide 46
Common Injection Molding Defects

## Slide 47: Co-Injection Moulding
Overmoulding
Preform is manufactured
Preform placed into the injection mould
Plastic moulded around / in the preform
E.G. Soft touch closures

## Slide 48: Injection over moulding

## Slide 49: Injection co moulding
Injection of two materials into same mould
Skin/core/skin formation
“Fountain flow” ensures skin is filled with core.
Skin material injected at end to prepare for next cycle.

## Slide 51: Compression Moulding

## Slide 52: Compression Moulding

## Slide 53: Compression Moulding
Charge
  Powder, paste or solid
Placed into heated mould and compressed
Shaped and polymerisation process completed

## Slide 54: EPS Moulding
EPS beads contain blowing agent
Pre blown with steam heating
Feed into mould
Blown and fused with heat.

## Slide 55: Extrusion Blow Moulding

## Slide 56: Extrusion Blow Moulding
Manufacture of hollow shapes, bottles drums etc.
Involved extrusion of parson, clamping in mould and blowing.
Cyclic operation

## Slide 57: Extrusion Blow Moulding
Parson extrusion
Clamping in mould
Inflation & cooling
Ejection from mould
Flash removal
Leak testing

## Slide 58: Extrusion Blow Molding

## Slide 59: Material Distribution

## Slide 60: Programmed Parson

## Slide 61: Mould Design
Hardened inserts at high wear areas
Must seal and can trim bottom
Provide for rapid cooling
Provide for air removal from cavity
Accurately locate mould halves.

## Slide 62: Features
Can be co-extruded
Can incorporate handles, and asymmetric design.
Moderate dimension tolerance
Cycle rate controlled by cooling time
Only require one lightweight mould

## Slide 63: Co-extrusion

## Slide 64: Injection Blow Moulding

## Slide 65: Injection Blow Moulding
Injection moulded parson or preform
Preform blown to produce container
Used for precision finishes, wide mouth containers etc.
Requires two moulds,- expensive set-up costs
No waste
Difficult to produce handles, co-extrusions

## Slide 66: Injection blow moulding

## Slide 67: Stretch Blow Moulding

## Slide 68: Stretch Blow Moulding
Blowing causes orientation in hoop direction
To provide bi-axial orientation must be stretched in longitudinal direction
Can be injection or extrusion stretch blow moulding

## Slide 69: Extrusion Stretch Blow Moulding

## Slide 70: Injection Stretch Blow Moulding

## Slide 71: Rotational Moulding

## Slide 72: Rotational Moulding Mould coating
Metal Mould for heat transfer
Polymer powder placed into mould
Mould transferred into oven & heated
  Mould rotated about 2/3 axis through
Polymer melted and coated onto inner surface
Mould cooled
  While being rotated
Opened and part removed

## Slide 73: Rotational Moulding
Slow process
Little waste, some finishing required
Think material layers
Cheap moulds
Only for complete vessels

## Slide 74: Rotational Moulding

## Slide 75: Thermoforming

## Slide 76: Thermoforming
Secondary shaping for sheet material
Simple shapes and designs
Low set up costs
Produces uneven material distribution
Widely used for trays, tubs, and inserts.

## Slide 78: Vacuum thermoforming

## Slide 79: Plug Assist Thermoforming

## Slide 80
Properties
Processes
Polymers