## Slide 1: Plastic Packaging
Plastic Polymerisation
Notes: Introduction
Welcome
Background to FPC
Important contribution to the food industry

## Slide 2: Contact
Tony Duffy
tony-duffy@outlook.com
++44(0)7526497265

## Slide 3: Plastic & Polymers
Plastic: Easily shaped or moulded
  Polymer: Poly (many) mer (parts)
  Monomer: Mono (one) mer (part)
Natural include cellulose, rubber, starch
Synthetic include most common plastics
  Derived from crude oil/gas
  Bio-based

## Slide 4: Plastic Production
4% of fossil fuel production goes into plastic
380 million tonnes produced per year
50% of plastic produced is used in packaging

## Slide 5: Plastic History
1200 BCE, Aztec used natural rubber
1820’s vulcanised rubber, cellulose
1869 Celluloid Billiard balls
1907 Bakelite – synthetic plastic
1937 Commercial Polystyrene production
1938 Commercial Nylon production
1945 Polyethylene squeezy bottle

## Slide 6: The Future is Plastic (1967)

## Slide 7: Production of monomers
Crude oil refined by fractionation
  Based on boiling points of materials
Cracking is used to fracture large molecules into smaller molecules which can be used to produce required components.

## Slide 9: Simple hydrocarbons
Methane CH4
Ethane C2H6
Propane C3H8
Butane C4H10
Pentane C5H12

## Slide 10: Alkenes (containing double carbon bonds)
Ethylene C2H4
Propylene C2H2CH3

## Slide 11: Monomers & Polymers

## Slide 12: Polymerisation Processes
Free radical addition polymerisation
Coordination addition polymerisation
Condensation polymerisation

## Slide 13: Addition Polymerisation

## Slide 14: Free radical initiation
Free radical: molecule fragment with unpaired electron
  E.g. Peroxides R-O-O-R
  Split into two free radicals R-O* *O-R
  Free radicals are reactive and will easily pair with other molecules

## Slide 15: Initiation and Propagation

## Slide 16: Process termination

## Slide 17: Coordination Initiation Ziegler Natta or metallocene
Catalysts (and co catalysts)provide reactive sites
  Titanium based
Reactions take place on the surface of the catalyst

## Slide 18: Propagation
Additional monomers attach themselves between the reaction site and the attached molecules.
Process continues for a large number of molecules forming long chains.
Can control arrangement of monomers

## Slide 19: Termination
Polymer chin becomes detached from catalyst and is no longer reactive.

## Slide 20: Polymerisation Processes
Free radical addition polymerisation
Coordination addition polymerisation
Condensation polymerisation

## Slide 21: Condensation Polymerisation
Reacts two monomers
Monomers have functional groups
  acids, alcohol, amine
Have 2 or more reactive sites
Monomers join and release a small molecule often water

## Slide 22: Nylon

## Slide 23: PET

## Slide 24: Cross Linking
Some monomers have three or more reactive sites.
Polymer chains can bond to reactive sites joining chains together.
Polymer chains can form a network of inter-linked chains.
Usually thermoset plasticsCrosslinking polymers with organic peroxides (youtube.com)

## Slide 25: Plastic types

## Slide 26: Plastic types Thermoplastics
Long molecules
Often carbon backbone
Independent polymer chains
Softens on heating
All common packaging plastics
  PE, PS, PP, PVC

## Slide 27: Plastic Types Thermoset
Polymer chains are cross linked (bonded)
Once polymerised shape is permanent
Will not soften with heat
Includes
  Epoxies, uera formaldhyde,

## Slide 28: Plastic Types Thermoplastic Elastomers (TPE)
Rubbery Thermoplastics materials
Blends or copolymers
Advantages of thermoplastics
Feel of thermoset elastomers.
  Styrene co-polymers
  Thermoplastic copolyester

## Slide 29: Break

## Slide 30: Modification of Polymers
Monomer
Molecular weight / distribution
Co Polymerisation
Tacticity
Chain Branching
Polarity
Crystallinity
Orientation

## Slide 31: Polymer properties
Monomer
Polyethylene C2H4
Polyvinyl chloride C2H3Cl
Polyvinylidene chloride C2H2Cl2
Polypropylene C2H3CH3
Polystyrene C2H3C6H5
Size of replacement group: Glass transition, stiffness crystallinity,

## Slide 32: Molecular weight
Molecular weight is size of polymer molecule.
How many monomers have been added to the polymer chain?
  Impacts on stiffness, melting point, viscosity (MFI)

## Slide 33: Molecular Weight Distribution
Measurement of distribution of molecular size
Narrow distribution
  Well defined properties e.g. melting temperature
Wide distribution
  Range of properties e.g. melting temperature

## Slide 34: Co-polymerisation
Co-polymer constructed from 2 or monometers
Arrangements can vary
  Block
  Random
  Alternating
  Graft
AAABBBBBAAABB
AABAABBBABB
ABABABABABABA
AAAAAAAAAAA
B
B
B

## Slide 35: Tacticity
3D arrangement of molecules e.g. PP
Atactic
  Random dispersion of methyl group
Isotactic
  All methyl groups on same side
Syndiotactic
  Methyl groups arranged on alternative sides

## Slide 36: Chain Branching
Polymer chains are not always straight chains.
Some side branches may be produced.
Amount of branching affects density

## Slide 37: Structure of Polyethylene

## Slide 38: Polarity
Non polar PE PP
  Low surface energy, repel water, inks adhesives
  Use corona treatment (or other ) to charge surface to attract ink
  Polar materials have regions of +ive charge and –ive charge
  -ive and +ive areas attract

## Slide 39: Crystallinity
Crystallinity is areas of structured tightly packed polymer chains
  Effects stiffness, permeability, opacity,

## Slide 40: Crystallinity
Amorphous Polymers
  random chains
Semi-Crystalline Polymers
  Ordered regions within amorphous mix
Effects
  Clarity, Stiffness, Permeability, Melting temperature

## Slide 41: Crystallinity

## Slide 42: Amorphous vs Crystalline plastic properties:

## Slide 43: Polymer Morphology
The Random Coil
  Polymer foetal position
Polymer Chain Branching
  e.g. HDPE, LDPE, LLDPE

## Slide 44: Orientation
Alignment of molecules
  Cold processes & Hot processes
Axial and biaxial
Properties
  Increased tensile strength, barrier properties,melting temperature

## Slide 45: Thermal Properties
Melting temperature (Tm)
Crystallization (Tc)
Glass transition (Tg)

## Slide 46: Heat Shrink Film
Heat polymer to allow some chain movement
Orientate by stretching
Rapid Cooling to “freeze” in structure
Re-heating to enable relaxation to random coil

## Slide 47: Stretch Film
Elastic properties of film

## Slide 48: Mixing Polymers
Co-Polymers
Blending / Compounding
Co-extrusion / Co-moulding
Laminating
Coating

## Slide 49: Plastic Performance Properties
Tensile strength
Tear strength
Impact strength
Heat seal-ability
C of F
Creep
Permeability
Transparency
Chemical resistance
Temperature range
  Glass transition
  Melt temperature