## Slide 1: Plastic Packaging
Plastic Characteristics
Notes: Introduction
Welcome
Background to FPC
Important contribution to the food industry

## Slide 2: What plastics do we use for packaging?

## Slide 3: Plastic Types
1 Polyethylene terephthalate (PET)
2 High density polyethylene (HDPE)
3. Polyvinyl chloride (PVC)
4. Low density polyethylene (LDPE)
5. Polypropylene (PP)
6. Polystyrene (PS)
7. Other

## Slide 4
Polyvinylidene chloride (PVDC)
Polyamide (Nylon)
Ethylene vinyl acetate (EVA) & ethylene vinyl alcohol (EVOH)
Polycarbonate (PC)
Polyethylene naphthallate (PEN)
Ionomers e.g. Surlyn
Fluoropolymers e.g. PTFE, Aclar
Styrene copolymers - SAN (styrene acrylonitrile) & ABS (acrylonitrile butadiene styrene)
High Impact Polystyrene
Cellulose film
Polylactic acid

## Slide 5: Mixing Polymers
Co-Polymers
Blending / Compounding
Co-extrusion / Co-moulding
Laminating
Coating

## Slide 6: Plastic Performance Properties
Tensile strength
Tear strength
Impact strength
Heat sealability
C of F
Creep
Permeability
Transparency
Chemical resistance
Temperature range
  Glass transition
  Melt temperature

## Slide 7: Polymer exercise
Key characteristics
  Clarity, temperature, strength, chemical resistance, barrier characteristics, limitations
Applications
  Rigid and flexible

## Slide 8: Target polymers
1 | PET | PEN
2 | HDPE | EVOH
3 | PVC | PVDC
4 | LDPE | LLDPE
5 | PP | Ionomer
6 | PS | PA
7 | PC | EPS
8 | PLA | HIPS
9 | SAN | PVOH

## Slide 9: Polyolefins (olefins, hydrocarbons)
Polyethylene
  HDPE, LDPE, LLDPE
    ULDPE, VLDPE
Ionomers
Metallocenes
Polypropylene

## Slide 10: High Density Polyethylene
Crystaline, linear with little branching.
Good moisture barrier
Poor gas barrier
Milky appearance
Cheap
Tough Strong and Stiff
Suffers from environmental stress cracking
Tg -125C, Tm 137C

## Slide 11: HDPE Applications
Flexible
  Boil in bag, sacks, bags,
Rigid
  Blow mounded milk bottles, household bottles, Drums, crates and tubs.

## Slide 12: Low Density Polyethylene
Branched structure
Good moisture barrier but poor gas barrier
Cheap
Good heat sealability
Resistant to most solvents
Soft, Flexible, Tough & Strong
Good transparency in thin sections

## Slide 13: LDPE Applications
Flexible
  Shrink film, stretch wrap, bags, sacks,
  Heat seal coating
Rigid
  Small bottles, snap on caps, threaded closures.

## Slide 14: Linear Low Density Polyethylene
Ethylene co-polymer with larger hydrocarbon
LLDPE Vs LDPE
  higher tensile strength and barrier than LDPE
  higher extensibility
  higher heat seal temperature
  better clarity
Notes: Copolymer with butene , hexene or octene

## Slide 15: LLDPE Applications
Flexible
Often blended with LDPE
  Stretch and shrink film, bags and sacks

## Slide 16: Ionomers (DuPoint-Surlyn)
Ethylene/Methacrylic acid co-polymer
Good grease & oil resistance
Improved clarity than LDPE
Lower water vapour barrier than LDPE
Good adhesion to foil
Main Application: Heat seal layer

## Slide 17: LDPE Metallocenes
Controlled polymerisation reaction
Narrow molecular weight distribution
Tailored for end use
  Increased clarity
  Increased toughness
  Difficult to process

## Slide 18: Polypropylene
Forms a living hinge
Good moisture & poor gas barrier
Tg -18C, Tm 176 C
Good strength & Stiffness but brittle at low temperatures
Slight opacity, but can be made clear in film,
Crankily, good chemical resiatance

## Slide 19: PP Applications
Flexible
  Wrappers for confectionery and bakery.
  Strapping
Rigid
  Closures and hinged closures, bottles trays, jars.

## Slide 20: Polystyrene
Amorphous with Benzene ring on main chain. Tg 90 C
Stiff, hard, brittle, poor strength
Very clear, high gloss
Resistant to acids & alkalis
Poor moisture & gas barrier
Easy to thermoform

## Slide 21: Expanded Polystyrene
Expanded polystyrene (EPS)
  Foamed
  Improved insulation, cushioning

## Slide 22: PS Applications
Breathable film
Carton windows
Yoghart pots, drinking cups
Clear covers containers etc.
Meat trays (EPS)
Cushions

## Slide 23: High Impact Polystyrene
High Impact Polystyrene (HIPS)
  Graft Copolymer Styrene-Butadiene
  Improved impact strength (x 7)
  Reduced clarity, strength

## Slide 24: ABS Acrylonitrile Butadiene Styrene
Similar to HIPS
Reduced water adsorption
More rigid

## Slide 25: SAN Styrene Acrylonitrile
Excellence clarity & Sparkle
Good resistance to fats and oil
More scratch resistance than GPPS
Improved gas barrier
Used for some cosmetic applications
Trade name Barex

## Slide 26: Polyvinyl Chloride
Unplasticised PVC
Plasticisied PVC
Environmental concerns
  Redidual monomer, plasticisers, disposal

## Slide 27: Unplasticised PVC
Usually Amorphous
Stiff hard brittle, poor impact resistance
Crystal clear
Good oil & grease barrier
Fair gas barrier but poor moisture barrier
Low operating temperature

## Slide 28: Rigid PVC Applications
Thermoformed trays e.g. sandwich trays
Biscuit trays/dividers, blister tablet packs
Water and juice bottles, Toiletries
Blood bags

## Slide 29: Flexable PVC
Soft
Elastic
Good cling
Applications
  Overwrapping, stretch wrapping

## Slide 30: Polyvinyidene Chlorine (PVdC)
Excellent gas and good water barrier
Good flavour & odour barrier
Good cling
Expensive
Applications
  Barrier layers or film, MAP, hot water shrink bags

## Slide 31: Polyethylene terephthalate
Fair water and gas barriers
Tg 69 C, Tm 267 C
Excellent chemical resistance
Good strength & stiffness
APET good clarity, CPET cloudy

## Slide 32: PET Applications
APET
  Soft drinks bottles, oil bottles, toiletries, roasting bags, laminates
CPET
  Ready meals trays , dual ovenable

## Slide 33: PETG Glycol modified PET
Glycol copolymer
Decreased crystallinity
Increased melt strength
Can be injection blow moulded.

## Slide 34: Polyethylene Napthalate (PEN)
Better barrier properties than PET
UV barrier
Expensive (4 times PET)
Used in a blend or copolymer with PET
Applications

## Slide 35: Polyamide (Nylon)
Condensation co-polymer
Characterised by number of carbon atoms in starting materials
Nylon 6, 6
Nylon 6
Nylon 11

## Slide 36: Polyamides (Nylon)
Excellent toughness
Poor moisture barrier
Good gas barrier
Heat resistant
Applications
  Vacuum bags for meat ( when laminated)

## Slide 37: Ethylene Vinyl Acetate (EVA)
Co-polymer
Similar to LDPE
Improved stretch, cling, and heat sealing
Applications
  Heat seal layers, improved stress crack resistance

## Slide 38: Polyvinyl alcohol (PVOH)
Excellent gas barrier
Chemical resistant, strong
Water soluble
Applications
  Laundry bags, chemical dosing, barrier layer

## Slide 39: Ethylene Vinyl Alcohol (EVOH)
Formed by hydrolysis of EVA
Outstanding barrier properties
Good grease, oil & aroma barrier
Moisture sensitive
Applications
  Barrier layer material

## Slide 40: Polycarbonate
Amorphous tough rigid polymer
Good clarity
Good moisture & Gas barrier
Sterilisable
Used for returnable containers.

## Slide 41: Fluoropolymers
PTFE (Teflon)
  Inert, high temperature, low friction
Polychlorotrifluoroethylene (Aclar)
  Good barrier and chemical resistance
  Coatings and laminates in pharmaceuticals

## Slide 42: Thermoplastic Elastomers (TPE’s)
Rubber type performance with thermoplastic process ability
High clarity good barrier tough film
Low extrables
Soft feel for grip on rigid materials
Medical devices, cap liners

## Slide 43: Bio-Plastics
Bio-based polymer is preferred term.
Does not relate to degradability

## Slide 44: Starch Based plastics
Thermoplastic materials
Modified with plasticizers e.g. glycerol
Can be blended with other biodegradable materials
Applications for film e.g. magazine wraps, bakery bags and compostable bags

## Slide 45: Cellulose
Bases on cellulose fibre
Excellent clarity.
Good deadfold
Poor moisture barrier

## Slide 46: Polylactic acid (PLA)
Reasonably common
Similar to PS
Degrades leaving no toxic residues

## Slide 47: Polyethylene Furanoate (PEF)
Possible replacement for PET
Some better characteristics
Not yet commercially avalilable.

## Slide 48: Poly-3-hydroxybutyrate (PHB)
Similar to PP
Produced into film with melting point 130oC
Degrades without residues
Not widely available

## Slide 49: Polyhydroxyalkanoate
Range of materials with medical applications
biodegradable

## Slide 50: Polyamide 11
Rilsan B trade name
Bio based polyamide
High performance applications

## Slide 51: Bio Polyethylene
Same as standard PE
Not degradable
Claimed to have lower carbon footprint

## Slide 52: Other Laminates / Coatings
Paper
Foil
Silica oxide (SiOx)

## Slide 53: Water vapor Transmission Rate

## Slide 54: Oxygen Transmission Rate