## Slide 1: Adhesives
How do adhesives work?
  Mechanical adhesion
  Chemical/Specific adhesion
  Diffusion
Definitions
Adhesive types and uses
Requirements for a good bond

## Slide 2: Samples Needed
A box of cereal – with the bag inside
A glass bottle with a plastic label
A glass bottle with a paper label
A chocolate bar
A bag of crisps

## Slide 3: How Adhesives Work (Mechanical Adhesion) – CEREAL BOX
Wet out the surfaces to be bonded
Penetrate the surfaces
Interlock with the fibres
Create mechanical links
Produce fibre tear

## Slide 4
Wetting Out - Basic Principle

## Slide 5: How Adhesives Work (Specific or Chemical Adhesion) Glass Bottle
Wet out the surfaces to be bonded
Adhesive is attracted to the substrate surfaces
Positive and negative charges occur at the substrate surface
Force of attraction is at the molecular level - Van der Waals forces

## Slide 6
Theories of Adhesion

## Slide 7: Lets talk about the Samples
A box of cereal – with the bag inside
A glass bottle with a plastic label
A glass bottle with a paper label
A chocolate bar
A bag of crisps

## Slide 8: Terminology
Viscosity
Tack
Open time
Setting time
Solids content

## Slide 9: Viscosity
The resistance of a fluid to flow
The higher the viscosity the greater the resistance to flow
Typical unit of measure is centipoise (cps) or millipascal second (mPa x s)

## Slide 10: Tack
The amount of stickiness
Resistance to pulling apart when adhesive is wet

## Slide 11: Open Time
Maximum amount of time between when an adhesive is applied and when the substrates can be brought together and still make an effective bond.

## Slide 12: Setting Time
The time from application of the adhesive to when an acceptable bond is developed.
This is usually the length of time that the bond must be under compression.

## Slide 13: Solids Content
What is left when the liquid carrier medium (water or an organic solvent) has dried.
Measured in %
  Hot melts are 100% solids, emulsions are about 50% solids and starch is about 30%.

## Slide 14: Types of Adhesive
Starch
Casein
Synthetic emulsions
Solvent based
Cold seal
Pressure sensitive
Hot melts

## Slide 15: Starch Adhesives
Made by chemical treatment of vegetable starches - maize, wheat, potato, Low solids content, Slow setting time, High tack
Withstand warm conditions
  good for labelling warm/hot containers
Not good in cold and wet conditions
  e.g. labelling cold bottles
Economical
  used in corrugated board making – what bond is this mechanical/chemical/diffusion?

## Slide 16: Casein Adhesives
Derived from the phosphoprotein in acidified milk. Absorb large quantity of water without significant change in viscosity good for applying labels to bottles in cold and wet conditions.
Very high tack -Good for applying labels to curved surfaces.
Good resistance in use to cold water
  e.g. labelling of bottles which will be cooled in iced water
  Chemical/mechanical/diffusion ?

## Slide 17: Synthetic Emulsions
Based on polymers
  eg. polyvinyl acetates, acrylates and maleates.
Solid adhesive particles are surrounded by a protective colloid, and the whole surrounded by water.
High solids ~ 50-75%

## Slide 19
How water based adhesives work
Starch/casein/water based emulsion
Set by the loss of water
Suspension breaks
Individual polymer ? units combine to form an adhesive film
Partial or green bond is formed
Bond strength increases as water evaporates

## Slide 20: How water based adhesives work
One substrate must be porous
e.g. Wet bond lamination of flexible packaging materials

## Slide 21: Solvent Based Adhesives
Used to combine single webs of flexible materials into required structure
Risk of retained solvent
Need for solvent recovery or solvent burning plant

## Slide 22: Dry Bond Lamination

## Slide 23: Pressure Sensitive Adhesives
Acrylic or rubber-type materials
Form instant bond
Can be peelable or permanent
Used on self adhesive labels

## Slide 24: Cold Seal Adhesives
Latex based
Only adheres to itself
Applied to the reverse of a printed film, in register to seal areas
Needs only pressure to bond
Does not give airtight seal

## Slide 25: Hot Melt Adhesives
Synthetic materials based on:
  Polymers - for strength
  Resins - for tack and adhesion
  Wax - as diluent
  Stabilisers
  Antioxidants
Thermoplastic - soften on heating, solidify on cooling

## Slide 26: Hot Melt Adhesives
100% solids - no solvent to dry
Fast setting - short compression time
Good for rough surfaces - fill gaps
Small space requirements
Immediate use of the pack
Limited heat resistance
Continuous energy requirement
Fuming & charring + burn hazard
Development of warm melts

## Slide 27
What happens as a Hot Melt cools
Time (secs)
Temp
°C
160
100
50
LIQUID
PLASTIC
SOLID

## Slide 28
O
OO
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
O
Emulsion
Hot Melt
SPEED
PENETRATION
HEAT RESISTANCE
WATER RESISTANCE
GAP FILLING
ADHESION
Starch
% Solids
30
55
100
Comparison of Starch/Emulsion/Hot Melt

## Slide 29: Requirements For a Good Bond
Apply just enough adhesive
Apply to correct place
Adhesive must wet out the substrate
Adhesive must be liquid (or molten) when substrates are brought into intimate contact

## Slide 30: Requirements For a Good Bond
Substrates must be held together until bond has formed
Temperature and humidity of factory and substrates affect setting time
Keep adhesive and applicator clean at all times

## Slide 31: What New ?
Plastics Tax – good news for adhesives
Cool Melts 170 to < 100
Bio Melts –ve CO2
Pop and Lock decreases use of plastics
Stitching